## Slide 1: Lecture 4b
Catalytic Air Oxidation with MoOxdtc2

## Slide 2: Introduction I
Metal complexes containing molybdenum in various oxidation states and with different ligands have gained a lot of interest in the past 40 years (i.e., molybdoenzymes)
  Molybdenum dioxo specie serve as model for oxidation
  Mo(IV) plays key role in reduction of nitrate
  Mo(IV) oxo compounds can coordinate alkenes, alkynes, etc. and can also deoxygenate epoxides

## Slide 3: Introduction II
In the lab, two molybdenum oxo dithiocarbamates (MoOxdtc2, x=1,2) are synthesized and tested as catalysts for the oxidation of benzoin
MoO2dtc2 is obtained by the reaction of Na2MoO4 with Nadtc in weakly acidic medium (NaOAc-HOAc buffer)
MoOdtc2 is obtained by the reaction of Na2MoO4 with Nadtc and Na2S2O4 (serves as reducing agent) via Mo2O3dtc4.

## Slide 4: Introduction III
Catalysis experiment (mechanism shown on the right, note that the nitrogen attached to Mo is a sulfur atom in our case)
  MoO2dtc2 is the oxygen transfer reagent
  The hydrated form of MoOdtc2 appears to be an intermediate
  Higher concentration of water make the loss of water in the intermediate less likely, which means that MoOdtc2 cannot be oxidized
  Under anaerobic conditions, MoOdtc2 undergoes an addition with MoO2dtc2 to form Mo2O3dtc4
  In addition, it can also undergo hydrolysis
????

## Slide 5: Experiment I
Cis-MoO2dtc2
  Sodium molybdate and sodium acetate are dissolved in water and diluted hydrochloric acid is added until a pH-value of 5.5 is reached (needs to be measured with a pH-meter!)
  The pH-value cannot be lower because the compound decomposes then (Mo2O3dtc4 (dark purple), etc.)
  The orange-brown crude isolated by filtration, washed and dried before being extracted several times with warm (50-60 oC) toluene
  The volume of the combined extracts is reduced and petroleum ether (or hexane) is added to precipitate the product

## Slide 6: Experiment II
MoOdtc2
  Note that this reaction has to be carried under strict Schlenk techniques
  Sodium molybdate and sodium dithionite are dissolved in deaerated water (freeze-pump-thaw)
  A dark purple precipitate is formed almost immediately (Mo2O3dtc4)
  Upon stirring, the color of the precipitate changes to pink within 2-3 hours
  The precipitate is isolated by filtration under inert gas, washed with deaerated water, deaerated ethanol and dry diethyl ether

## Slide 7: Experiment III
Catalytic experiments
  The Mo-compounds are tested as catalysts in the air oxidation of benzoin
  PhCH(OH)COPh + ½ O2 PhCOCOPh + H2O
  Each experiment uses 1 mmol of benzoin and 0.05 mmol of the catalyst (cis-MoO2dtc2, MoOdtc2, cis-MoO2dtc2 with molecular sieve, no catalyst (as control))
  Solvent: dry DMF (has to be prepared by the student)
  In order to assess the kinetics, one sample is removed after 2 hours. The reaction is stopped after 24 hours by adding water!
  Quantitation is performed with GC (~5 mg/mL)

## Slide 8: Characterization I
Infrared spectroscopy
  The infrared spectra are acquire using the FTIR instrument (ATR) in YH 6076 and the instrument in YH 1033 (Nujol/CsI)
  Cis-MoO2dtc2
    n(C-N)= 1524 cm-1
    n(C-S) = 993, 1010 cm-1
    n(Mo=O)= 883 and 915 cm-1
    n(M-S)= 390 cm-1
  MoOdtc2
    n(C-N)= 1536 cm-1
    n(C-S) = ~1000 cm-1
    n(Mo=O)= 962 cm-1
    n(M-S)= 380 cm-1

## Slide 9: Characterization II
EPR
  Measured in dry dichloromethane in EPR tube (which is made from quartz and 4 mm in diameter and longer than a NMR tube)
  MoOdtc2 contains Mo(II), which possesses a d2-configuration
    Two different ground states possible resulting in no unpaired electron or two unpaired electron
    All electrons paired: no EPR signal
    Two unpaired electrons: EPR signal observed
  If the compound is partially oxidized with air, Mo2O3dtc4 is formed, which contains paramagnetic Mo(V), which possesses a d1-configuration
  The complete oxidation leads to the formation of MoO2dtc2, which contains Mo(VI), a d0-configuration which is diamagnetic